EarthGuard® Fiber Matrix

Special Provisions

THE SPECIAL PROVISIONS DESCRIBED WITHIN IS AN ATTEMPT TO COVER MOST DESIGN ASPECTS OF UTILIZING THE EARTHGUARD FIBER MATRIX EROSION CONTROL SYSTEM. THIS DOCUMENT IS INTENDED TO BE UTILIZED AS A GUIDELINE, WHICH CAN BE CUSTOMIZED BY THE USER TO MEET SPECIFIC PROJECT REQUIREMENTS.

THIS PROVISION DOES NOT ATTEMPT TO ADDRESS ALL ASPECTS OF EROSION CONTROL DESIGN. A PROFESSIONAL ENGINEER RESPONSIBLE FOR DESIGN SHOULD CHECK THE INFORMATION PRESENTED IN DETAIL. CONSULT YOUR EARTHGUARD REPRESENTATIVE FOR MORE INFORMATION.

SOME SITUATIONS WITH: SANDY-SANDY LOAM SOILS, VERY LITTLE ORGANIC MATTER IN THE SOIL, POORLY COMPACTED SLOPES, HEAVY RAINFALL LOCATIONS (OVER 20” or 500 mm PER YEAR), VERY INTENSE RAIN STORMS (50-75 MM AT A TIME), HIGH WIND EXPOSURE, ETC. MAY REQUIRE INCREASING THE APPLICATION RATES. WHEN SWPPPS, BMPS OR OTHER PLANS ARE BEING WRITTEN, CONTACT YOUR EARTHGUARD REPRESENTATIVE AT (888) 843-1029 FOR MORE SPECIFIC RATE RECOMMENDATIONS BASED ON SOIL TYPE, RAINFALL, SLOPE AND OTHER CONDITIONS.

PLEASE CONTACT TERRA NOVO INC.:

PHONE: 888-843-1029

EMAIL: SALES@TERRANOVO.COM

WEBSITE: WWW.EARTHGUARD.COM

1. GENERAL

1.1. Work Included. EarthGuard Fiber Matrix shall be furnished and applied as shown on the drawings and as required for proper installation and functioning of the product. The product is manufactured in liquid form that can be added to standard fiber mulch or is packaged in a 50 lb bag with the EarthGuard chemistry inside.

2. MATERIALS

2.1.A.  EarthGuard Liquid Soil Stabilizing Blend. The soil stabilizing emulsion blend to be applied shall be “EarthGuard” as manufactured by Terra Novo Inc. (888) 843-1029. It must be a true emulsion consisting of two completely immiscible liquids, in which minute globules of one liquid are dispersed but not dissolved throughout the other liquid.

The soil stabilizing emulsion blend to be used shall consist of at least (3) three different linear anionic copolymer of acrylamide/sodium acrylate emulsions, lending distinct molecular weights greater than 12x106 and anionic mole percentages (charge density) greater than 25%, within one emulsion. The blend must be guaranteed to contain 30% (+/- 1%) active polymer, in which all of the active particles are ultra-fine in size. The blend shall also be guaranteed to have 500 ppm or less of residual acrylamide.

The soil stabilizing emulsion shall be nontoxic to plant and animal life. It must also be registered and licensed by the State of California, Department of Food and Agriculture, as an “auxiliary soil amendment.”

EarthGuard can be stored for 12 months. Always thoroughly mix before using. Always close or seal containers after use. Store in a dry insulated location to avoid moisture and freezing. If frozen, thaw and completely remix the solution.

A Certificate of Compliance for the EarthGuard liquid shall be furnished to the Engineer.

EarthGuard liquid, when applied with fiber mulch, shall be applied with either one of the following types of fiber mulch:

2.1.A.1. Wood Fiber Mulch

The sterilized weed-free wood fiber mulch shall be manufactured through a thermo-mechanical defibrating process containing a specific range of fiber lengths averaging 0.25 inches or longer.  The fibers shall be dyed with a green water-soluble non-toxic dye that will not stain masonry, concrete, asphalt or painted surfaces, and shall be non-toxic to plant or animal life.

The wood fiber shall meet the following requirements:

- Fiber Retention On 28-Mesh Screen (Tyler Ro-Tap Method)         	≥ 40%

- EcoToxicity 								Non-Toxic (EPA 821/R-02/012)

- Moisture Holding Capacity 						1200% (minimum)

- Non-Toxic To Plant Or Animal Life                                                         	YES

- Sterilized Weed-Free							YES

- Biodegradability 								100%

A Certificate of Compliance for the wood fiber shall be furnished to the Engineer.

2.1.A.1. Wood/Cellulose Fiber Mulch Blend

The sterilized weed-free fiber mulch blend shall consist of 100% virgin wood fiber and post-consumer recycled cellulose fiber thermomechanically processed wood fiber mulch shall be manufactured through a thermo-mechanical defibrating process containing a specific range of fiber lengths averaging 0.25 inches or longer.  The fibers shall be dyed with a green water-soluble non-toxic dye that will not stain masonry, concrete, asphalt or painted surfaces, and shall be non-toxic to plant or animal life.

The wood fiber shall meet the following requirements:

- Thermo-Mechanically Processed Virgin Wood Fiber 			70%

- Post-Consumer Recycled Cellulose Fiber 			 	≤ 30%

- Moisture Holding Capacity                                                            	1100% Min

- Non-Toxic To Plant Or Animal Life                                                         	YES

- Sterilized Weed-Free							YES

- Biodegradability 								100%

A Certificate of Compliance for the wood/cellulose fiber shall be furnished to the Engineer.

2.1.B.  EarthGuard Fiber Matrix Pre-Packaged

“EarthGuard Fiber Matrix” shall be manufactured by Terra Novo Inc. (888) 843-1029. EarthGuard Fiber Matrix shall be pre-packaged in 50 lb bags containing both a proprietary compound of soil/fiber stabilizing chemistry and thermally processed wood fiber to assure both material performance and compliance with the following values. The Proprietary Linear Soil and Fiber Stabilizing Compound shall be pre-packed within the bag having a minimum content of 1.0%

The thermally processed wood fiber shall meet the following requirements:

- Thermo-Mechanically Processed Virgin Wood Fiber 			100%

- Moisture Holding Capacity                                                            	1400% Min

- Non-Toxic To Plant Or Animal Life                                                         	YES

- Sterilized Weed-Free							YES

- Biodegradability 								100%

A Certificate of Compliance for the Pre-Packaged EarthGuard Fiber Matrix product shall be furnished to the Engineer.

2.2. Seed (OPTIONAL – SPECIFY TYPE IF REQUIRED). The seed to be applied in combination with the EarthGuard Fiber Matrix shall be of Type __________________ as shown in the plans and specified within these Special Provisions.

## Seed shall be labeled by the vendors supplying the seed. Seed shall have been tested for purity and germination not more than 12 months prior to the application of the seed. Seed testing results shall be delivered to the Engineer prior to applying the seed. Seed labels furnished by the seed supplying vendor shall indicate the purity, germination and pure live seed as determined by testing.

Seed with a germination rate lower than the minimum rate specified may be used when approved by the Engineer in writing.

Seed specified without a germination requirement, at the time of sowing, shall be from the previous or current year's harvest, and shall be labeled to include the name date (month and year) collected and the name and address of the seed supplier.

2.3. Fertilizer (OPTIONAL – SPECIFY TYPE IF REQUIRED). The fertilizer to be applied in combination with the EarthGuard Fiber Matrix shall be __________________ as shown in the plans and specified within these Special Provisions.

3. EARTHGUARD FIBER MATRIX

EarthGuard Fiber Matrix shall be mixed in the following proportions depending on which product is utilized, liquid or pre-packaged. Seed can be added to the blend for long-term or permanent erosion control. Consult your EarthGuard Sales Representative and/or product manufacturer Terra Novo Inc. at (888) 843-1029 for the appropriate project specific application rates.

3.1. Normal Conditions. Use Chart 1A & 1B when the project requires a service life of EarthGuard Fiber Matrix to withstand up to 20” of rain over a period of time.

Chart 1A: EarthGuard (Liquid) Fiber Matrix+

| Maximum Rainfall of ≤ 20" |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SLOPE | 6:1 | 5:1 | 4:1 | 3:1 | 2:1 | 1½: to 1 | 1:1 |
| EARTHGUARD (gals/acre) | 4 | 5 | 6 | 7 | 8 | 9 | 10 |
| EARTHGUARD (liters/hectare) | 37.4 | 46.8 | 56.1 | 65.5 | 74.8 | 84.2 | 93.5 |
| Fiber (lb/acre) | 1500 | 1500 | 1500 | 1800 | 2000 | 2500 | 3000 |
| Fiber (kg/hectare) | 1680 | 1680 | 1680 | 2020 | 2245 | 2810 | 3355 |

Chart 1B: EarthGuard (Pre-Packaged) Fiber Matrix+

| Maximum Rainfall of ≤ 20" |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| SLOPE | ≤ 4:1 | 3:1 | 2:1 | 1½: to 1 | 1 to 1 |
| Pre-Packaged (lb/acre) | 1500 | 1800 | 2000 | 2500 | 3000 |
| Pre-Packaged (kg/hectare) | 1680 | 2020 | 2245 | 2810 | 3355 |

3.2. Severe Conditions. Use Chart 2A & 2B when the project requires a service life of EarthGuard Fiber Matrix to withstand over 20” of rain over a period of time.

Chart 2A: EarthGuard (Liquid) Fiber Matrix+

| Maximum Rainfall of > 20" |  |  |  |
| --- | --- | --- | --- |
| SLOPE | ≤ 5:1 | 4:1 | ≥ 3:1 |
| EARTHGUARD (gals/acre) | 6 | 8 | 10 |
| EARTHGUARD (liters/hectare) | 56.1 | 74.8 | 93.5 |
| FIBER (lb/acre) | 2000 | 2500 | 3000 |
| Fiber (kg/hectare) | 2245 | 2810 | 3335 |

Chart 2B: EarthGuard (Pre-Packaged) Fiber Matrix+

| Maximum Rainfall of > 20" |  |  |  |
| --- | --- | --- | --- |
| SLOPE | ≤ 5:1 | 4:1 | ≥ 3:1 |  |
| Pre-Packaged (lb/acre) | 2,000 | 2,500 | 3,000 |  |
| Pre-Packaged (kg/hectare) | 2245 | 2810 | 3335 |  |

+ SOME SITUATIONS WITH: SANDY-SANDY LOAM SOILS, VERY LITTLE ORGANIC MATTER IN THE SOIL, POORLY COMPACTED SLOPES, HEAVY RAINFALL LOCATIONS (OVER 19 INCHES PER YEAR), VERY INTENSE RAIN STORMS (2-3 INCHES AT A TIME), HIGH WIND EXPOSURE, ETC. MAY REQUIRE INCREASING THE EARTHGUARD AND/OR FIBER RATES.

4. BLENDING

Correct mixing and proper application are key factors in obtaining satisfactory performance. Engage agitators at ¾ speed. Fill hydroseeding vessel with water to at least 1/3 capacity (high enough to cover agitators) prior to adding any EarthGuard Fiber Matrix. Continue to fill vessel with water and slowly add the EarthGuard Soil Emulsion or EarthGuard Fiber Matrix while agitators are in motion. Once the accurate amount of EarthGuard Fiber Matrix is loaded, add seed (if specified), and fertilizer (if specified). Continue to mix tank a minimum of 10 minutes prior to application.

If the hydroseeding unit has separate pump and agitator controls (example: Finns), minimize agitator speed once the slurry is completely mixed and before application so that the agitators are barely rotating. This will help increase application rate.

5. APPLICATION AND LOADING INSTRUCTIONS

The soil to which the EarthGuard Fiber Matrix slurry shall be applied to must be graded to remove any pre-existing rills and shall be compacted to meet project specifications. Track-walking or some other soil imprinting devise is recommended to roughen the slope to slow water flows during a storm event. Slope Interruption Devices, such as fiber rolls, should be applied prior to the application of EarthGuard Fiber Matrix if desired.  Slope Interruption Devices, if installed should be placed on the slope contour perpendicular to the flow of water.

Loading Instructions:

- Fill vessel to at least 1/3 capacity (high enough to cover agitators).

- Turn on agitators, place in reverse gear, and adjust to ¾ speed rate.

- Continue to fill vessel with water and slowly add the EarthGuard while agitators are in motion.

- Once the accurate amount of EarthGuard is in a slurry solution, add seed (if specified), compost (if specified), fertilizer (if specified) and pre-emergent (if specified).

- Continue to mix tank a minimum of 10 minutes prior to application. Toggle between forward and reverse gears to properly mix slurry. Maintain agitator speed at ¾ rate or slightly above.

- If the hydroseeding unit has separate pump and agitator controls (example: Finns), minimize agitator speed once the slurry is completely mixed and before application. This will help increase application rate.

- Place agitators in forward gear and begin application.

Caution should be taken to avoid creating puddles or runoff. It is recommended for the slurry to be sprayed from multiple directions and angles to ensure proper coverage. Treated areas shall not be disturbed after application.

It is recommended that EarthGuard Fiber Matrix be applied 24 hours prior to or following a storm event if possible.

6. REPAIR OF DAMAGED AREA

Any damaged area shall be repaired utilizing the exact blend and application procedure as specified above.

7. PAYMENT

EarthGuard Fiber Matrix will be paid for by the square foot (square meter) of area treated. The price shall include full compensation furnishing all labor, materials, tools, equipment, and incidentals, and for doing all EarthGuard Fiber Matrix work, complete in place, as shown on the plans, and as specified in these special provisions, and as directed by the Engineer.